## Slide 1: ALUMINIUM ALLOY L81

## Slide 2: APPLICATIONS
Nameplates, traffic (road) signs,architectural paneling. Welded tubes, chemical industry, irrigation. Offshore applications, welded structures. Pressure vessels, boilermaking.
Characteristic Properties:
Very good corrosion resistant to seawater and marine and weldability. Medium to high strength alloy for sheet products slightly lower than 5086. Medium high fatigue strength. Good cold formability.

## Slide 3: CHEMICAL COMPOSITION
CHEMICAL ELEMENT
Titanium(Ti)
Iron(Fe)
%PERSENT
0.0 – 0.15
Chromium(Cr)
Copper(Cu)
Zinc(Zn)
Magnesium(Mg)
Silicon(Si)
Maganese(Mn)
Aluminium(Al)
0.0 – 0.50
0.0 – 0.15
0.0 – 0.15
0.0 – 0.15
0.10 – 0.50
1.70 – 2.40
0.0 – 0.40
Balance

## Slide 4: PROPERTIES
Physical property
Density
Value
Melting point
Thermal Expansion
Modulus of Elasticity
Thermal Conductivity
Electrical Resistivity
2.69 g/cm3
650 C
23.6 * 10^-6 /K
70.0 Gpa
149 W/m.K
37.5 % IACS

## Slide 5: SHEET – 0.4mm to 0.8mm
Mechanical Property
Value
225 Min – 275 Max N/mm2
Tensile Strength
0.2% Proof Stress
Elongation A50mm
175 Min N/mm2
3 Min %

## Slide 6: ALLOY DESIGNATIONS
Aluminium alloy BS L81 – 5251 is covered by standad BS EN 3L81 (1985)